## Slide 1: Lecture 18
Superconductivity

## Slide 2
Superconductivity
Perfect diamagnetism
Perfect conductivity

## Slide 3: What we will learn
Diamagnetic character
Microscopic origin (Cooper pair, BCS)
Macroscopically coherent quantum state (BEC)
Current density and wave function
Different types of superconductors
Flux quantization

## Slide 4
Diamagnetism??
Anti-parallel!

## Slide 5: Meissner Effect (perfect diamagnet)
http://www.fys.uio.no/super/levitation/

## Slide 6: Essential Characteristics
RESISTANCELESS CONDUCTION
Temperature
Resistivity
0
Metal
Superconductors
Tc
1911 K. Onnes Superconductivity in Hg
MEISSNER EFFECT:
Perfect diamagnetism
1933 Meissner effect

## Slide 7: Understanding of Superconductivity
Year of Discovery
Transition Temperature (K)
1950 Isotope effect Tc~M-a (a~1/2)
1957 BCS Theory
(Bardeen, Cooper, Schrieffer)
BCS Theory
1962 Tunneling experiments

## Slide 8
BCS theory
e
+Z
+Z
+Z
+Z
e
PHONON MEDIATED PAIRING
(phonon = lattice vibration)
Pairs of electrons: Cooper pairs
Tc~wph exp(-1/l)~M-1/2
El-ph coupling constant: l
Superconducting gap: D
e-ph wins e-e at low freq. (Slow Wins!)
M

## Slide 9: How many electrons participate?
Not all electrons can participate in Cooper pairing.
In quantum mechanical view, the interaction described in the previous slide is described as two electrons exchanging a phonon (lattice vibration quantum).

## Slide 10: How many electrons participate?
Only those electrons near form Cooper pairs. These are the electrons
with energies where is the Debye frequency (typical frequency for phonons). Why? Due to Pauli exclusion principle, electrons cannot scatter by absorbing or emitting a phonon when they are deep inside the Fermi sea (). So, only a fraction, , of total electrons participate in Cooper pairs.

## Slide 11
Superconductivity – Dance of Electron Pairs
Phys. Today, March ‘04
Origin of SC = PAIRS dancing to the SAME tune
Notes: So, I described to you what is the phenomenology of the superconductivity.
But, what is the microscopic origin?
Regardless of conventional or high temperature superconductivity, researchers agree on one aspect.
Namely, the superconductivity is due to pairing of two electrons.
In this illustration, a female person symbolizes an electron with one spin quantum number and a male person symbolizes another electron with the other spin quantum number.
Then, the superconducting state is a state in which each female and each male are happily paired together and dancing together in a sort of harmonious and happy fashion.
Of course, in this illustration, it is not noted just what is pairing these two electrons.

## Slide 12: Superconducting Order Parameter (Ginzburg-Landau; Gorkov)
Can be viewed as the “wave function” of the condensate (i.e. ALL electron pairs)
All electron pairs (Cooper pairs) have the same wave function, in particular the same phase (like photons in laser)

## Slide 13: What does it really mean that all pairs have the same wave function?
Identical particles
  All electrons (fermions) are indistinguishable in quantum mechanics.
  All electron pairs – Cooper pairs – (bosons) are indistinguishable in quantum mechanics.
When identical bosons “condense”, we got a Bose-Einstein condensation.  Superfluid (no charge), Superconductor (charge)
A quantum state with macroscopic coherence

## Slide 14: What does it really mean that all pairs have the same wave function?
All bosons in the same wave functions.
A crude analogy is the vibrations in a guitar string or an ocean wave or any similar wave phenomenon. (Although such systems are not quite clean enough. Laser is a much better analogy.)
A large amplitude in a wave means many quanta of vibrations – many bosons!
Can we distinguish one vibration quantum from another when a guitar string vibrates? No. Such a state must be viewed as collective.
Except that in superconductors, these indistinguishable bosons are “tangible stuff” electron pairs – so, it is mind-boggling…
A quantum state with macroscopic coherence (all = one)

## Slide 15: So How does it work?
London Equation
cgs unit
Meissner Effect
Infinite Conductivity
Cooper Pair
Hamiltonian in presence of A

## Slide 16: Two Length Scales and two types of SC

## Slide 17: Two Length Scales and two types of SC
Type II
Type I

## Slide 18: Two types of SC

## Slide 19: Flux quantization
The wave function is fine for a linear superconductor. But, how about in general, e.g., for a ring of superconductor? must be a function of position, .
Then, the charge flux (from slide 14; SI unit now).
In the interior of the ring superconductor, (as ), and so .

## Slide 20: Flux quantization
The magnetic flux is given by
  due to and Stoke’s theorem.
This and means that . But where is an integer, since the spatial wave function must be single-valued. Thus
Tesla